R10 	RAINWATER DRAINAGE SYSTEMS

## 325 	Composite Gutter

-   	Manufacturer and reference: CGL Systems Ltd, 2 Young Place, Kelvin Industrial Estate, East Kilbride, G75 0TD.

Tel: 01355 235 561, Fax: 01355 247 189

E-mail: web@cglsystems.co.uk

-    	CGL Systems Ltd Composite Gutter - A prefabricated light-weight self-supporting metal composite insulated construction with a fully bonded, continuous membrane lining to the water-carrying surface.  The gutters are suitable for regular walkway traffic and have minimal maintenance requirements. CGL can provide design and specifications for a full RainPulse Rainwater Management service, and it is recommended that they are consulted early in the design process.

-   	Profile: Valley / Box / Boundary wall (Select)

- Type: CGL Systems Ltd Membrane Lined Gutter as part of the CGL RainPulse Rainwater Management System.

- Construction:

External Finish - 1.2mm thick PVC weatherproofing membrane, colour: Light grey.  Factory laminated to 0.6mm/0.9mm or 1.2mm thick galvanised steel to BS EN 10142 grade Fe P02G with Z275 coating.

Insulation – 90mm Polyisocyanurate (PIR) which is CFC and HCFC free providing a “U” value of 0.25 W/m²K. (For alternative “U” values consult with CGL Systems Ltd).

Internal Liner Sheet –

0.7mm thick Polyester coated White Enamel, 20 micron top coat to underside of lining.

-   	Nominal Size(s):  ……mm Girth.  (Consult with CGL Systems Ltd and Insert Sizes).

-   	Accessories:

CGL RainPulse Rainwater Outlets: fitted on site at appropriate locations within the CGL Systems Ltd Gutter.

CGL RainPulse Downpipe System: fitted to CGL Rainwater Outlets on site.  Downpipes either HDPE or Aluminum mill finish or with PPC finish.

Tell tale overflows fitted either in the gutter base or the stop ends.

Support where required: Loose pre-galvanized steel support straps 50 x 6mm flat bar to BS 4360, galvanized to BS 729

-   	Site fixing materials: 4.9mm diameter plated steel rivets, Outlets and overflows which are generally supplied loose for site installation and positioning.

-   	Factory fabricated: Fitted stop ends / mitered corner sections / tee sections / change of section / sumps.

-   	Method of jointing: Form site joints and fit outlets and overflows by riveting the overlap of metal and hot air weld overlapping PVC membrane, leaving a central unbonded strip which allows for expansion and contraction.

-   	Method of fixing: Gutter wings to be pre-fixed to purlin / support steelwork at approximately 300mm centre’s both sides prior to installation of roof liner sheet.

335	Single Skin Gutter

-   	Manufacturer and reference: CGL Systems Ltd, 2 Young Place, Kelvin Industrial Estate, East Kilbride, G75 0TD.

Tel: 01355 235 561, Fax: 01355 247 189

E-mail: web@cglsystems.co.uk

-	CGL Systems Ltd Single Skin Gutter - A prefabricated metal profile with a fully bonded, continuous membrane lining to the water-carrying surface.  The gutters are suitable for regular walkway traffic and have minimal maintenance requirements.  CGL can provide a design and specifications for a full RainPulse Rainwater Management service.

-   	Size(s):  (insert……mm) Girth. (Consult with CGL Systems Ltd and insert sizes).

-	Gutter construction:

External finish: 1.2mm thick PVC weatherproofing membrane, colour: Light grey.

Metal finish: 1.2mm / 1.6mm / 2mm / 3mm thick galvanized steel to BS EN 10142 grade Fe P02G with Z275 coating. (Consult with CGL Systems Ltd and insert thickness)

-	Method of jointing: Form site joints and fit outlets and overflows by riveting the overlap of metal and hot air weld overlapping PVC membrane, leaving a central unbonded strip which allows for expansion and contraction.

-	Method of fixing: Gutter wings to be pre-fixed to purlin/support steelwork at approximately 500mm centers both sides prior to installation of roof liner sheet.

-	Accessories:

CGL RainPulse Rainwater Outlets fitted on site at appropriate locations within the CGL Systems Ltd Gutter.

CGL RainPulse Downpipe System fitted to CGL Rainwater Outlets on site.  Downpipes either HDPE or Aluminum mill finish or with PPC finish.

Tell tale overflows fitted either in the gutter base or the stop ends.

Support where required: Loose steel support straps 50 mm x 6mm flat bar to BS 4360, galvanized to BS 729 
Gutter Site fixing materials: 4.9mm diameter plated steel rivets, outlets and overflows which are generally supplied loose for site installation and positioning.
Factory fabricated: Fitted stop ends / mitred corner sections / tee sections / change of section / sumps.

- Method of fixing: Gutter wings to be pre-fixed to purlin/support steelwork at approximately 500mm centres both sides prior to installation of roof liner sheet.

- Accessories:

CGL RainPulse Rainwater Outlets fitted on site at appropriate locations within the CGL Systems

CGL RainPulse Downpipe System fitted to CGL Rainwater Outlets on site. Downpipes either HDPE or Aluminum mill finish or with PPC finish.

Tell tale overflows fitted either in the gutter base or the stop ends.
Gutter Site fixing materials: 4.9mm diameter aluminium rivets, outlets and overflows which are generally supplied loose for site installation and positioning.
Factory fabricated: Fitted stop ends / mitred corner sections / tee sections / change of section / sumps

345   	Gutter Liner

-  	Manufacturer and reference: CGL Systems Ltd, 2 Young Place, Kelvin Industrial Estate, East Kilbride, G75 0TD.

Tel: 01355 235 561, Fax: 01355 247 189

E-mail: web@cglsystems.co.uk

-	CGL Systems Ltd Gutter Liner - A prefabricated metal profile with a fully bonded, continuous membrane lining to the water-carrying surface. The liner is designed to be used on failed existing gutters or during a building refurbishment. CGL can provide a design and specifications for a full RainPulse Rainwater Management service, and it is recommended that they are consulted early in the design process.

-   	Size(s):  (insert……mm) Girth.  (Consult with CGL Systems Ltd and insert sizes).

-   	Gutter construction:

External finish: 1.2mm thick PVC weatherproofing membrane, colour: Light grey.

Metal finish: 0.6mm thick galvanised steel to BS EN 10142 grade Fe P02G with Z275 coating.

- Method of jointing: Form site joints and fit outlets and overflows by riveting the overlap of metal and hot air weld overlapping PVC membrane, leaving a central unbonded strip which allows for expansion and contraction.

- Method of fixing: Gutter wings to be pre-fixed to purlin/support steelwork at approximately 500mm centres both sides prior to installation of roof liner sheet.

- Accessories:

CGL RainPulse Rainwater Outlets fitted on site at appropriate locations within the CGL Systems Ltd Gutter.

CGL RainPulse Downpipe System fitted to CGL Rainwater Outlets on site.  Downpipes either HDPE or Aluminum mill finish or with PPC finish.

Tell tale overflows fitted either in the gutter base or the stop ends.
Gutter Site fixing materials: 4.9mm diameter aluminium rivets, outlets and overflows which are generally supplied loose for site installation and positioning.
Factory fabricated: Fitted stop ends / mitred corner sections / tee sections / change of section / sumps